14oz BRIGHTWEAVE SPECIFICATIONS

| Style # | 19215-BW |
| --- | --- |
| FIBER CONTENT/FINISH | Vinyl Coated Polyester with Abrasion Resistance |
| CONSTRUCTION | 36 x 15 Woven |
| DENIER | 500 |
| WEIGHT (ASTM D-3776) | 13.9 oz/yd2 |
| THICKNESS | 0.0329 in |
| TENSILE STRENGTH (ASTM D-5035) | Warp: 268.5 lbf Fill: 125.8 lbf |
| TENSILE ELONGATION (ASTM D-5035) | Warp: 13.9% Fill: 11.1% |
| TRAPEZOIDAL TEAR STRENGTH (ASTM D-4533) | Warp: 92.9 lbf Fill: 39.8 lbf |
| FLAMMABILITY RATING | CA 117-2013, CS 191-53 |
| WEATHERABILITY (G154) | 1,200 Hours |
| AVAILABLE WIDTH(S)* | 36”, 48” |
| AVAILABLE COLOR(S) | Orange |
| Technical data provided by producing mill for first quality run of equivalent product. Results will vary with Seconds. Values are subject to updating at the sole discretion of Acadian Inc. Buyer is responsible for verifying the suitability of product for a particular application. In no event will Acadian Inc.’s liability for any sale exceed the purchase value of the product as invoiced for that sale. Acadian, Inc will never be liable for loss of profit, special, indirect, or consequential damages. |  |

*Call for currently available widths

Additional options may be available*